MIEC FULL RIVER CAP.CO.,LTD

No.7 alley 211 lane 126 , Hsi Nan Road Sec.1 Wujih Taichung , Taiwan R.O.C.414

TEL：886(04)23352688 FAX：886(04)23352168 EMAIL：lingin.ec@msa.hinet.net

Power Type MPL Series

Features

Passive Balanced Cells

Higher Voltage Rating

RoHS compliant

Recommended Applications

Hybrid Battery Packs

Stereo and Audio System

Battery Alternatives

Renewable Energy Systems

Specification

IRated Voltage           5.4 V

Surge Voltage            5.7 V

Capacitance Tolerance   -20 ％ / +20 ％

Operating Temperature   -40 ℃ to 65 ℃

Storage Temperature     -40 ℃ to 70 ℃

Endurance             △C Within ±30% of initial measured value

1000hr @65℃ at Rated Voltage

ESR Within 2 times of initial specified value

Life time               10y @ 25 △C Within ±30% of initial measured value ℃at Rated Voltage

ESR Within 2 times of initial specified value

500k cycles △C Within ±30% of initial measured value

Cycle Life              ESR Within 2 times of initial specified value

Cycle: between specified voltage and half voltage under constant current at 25℃

Dimensions

| A | B | C | d | F |
| --- | --- | --- | --- | --- |
|  |  |  | 0.6 |  |

Standard RatingsL d F a

| Rated Cap(F) | Size mm | Internal Resistance （mΩ） | LC (mA) | Stored Energy | Specific Energy | Specific power | Max. Current | ISC | Weight | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Measure At 25℃ | ΦDXL | AC (1KHz) | DC | 72Hrs 25℃ | Wh | Wh/kg | Wh/L | Pd W/kg | Pmax W/kg | 1s to 1/2V(A) | (A) | (g) | MPL5R4155 |
| 1.5 | 11*21*24 | 300 | 580 | 0.15 | 0.0061 | 1.3500 | 1.9347 | 1341 | 5400 | 2.17 | 9.31 | 4.5 |  |