MIEC  FULL RIVER CAP. CO.,LTD

No.7 alley 211 lane 126 , Hsi Nan Road Sec.1 Wujih Taichung , Taiwan R.O.C.414

TEL：886(04)23352688 FAX：886(04)23352168 EMAIL：lingin.ec@msa.hinet.net

Power Type  NL Series

Features

High capacitance and low-resistance

Quick charge & discharge

Environmentally friendly products

Recommended Applications

Pulse power demand

Hybrid battery packs

Power tools

Specification

IRated Voltage           2.7 V

Surge Voltage            2.85 V

Capacitance Tolerance   -20 ％ / +20 ％

Operating Temperature   -40 ℃ to 65 ℃

Storage Temperature     -40 ℃ to 70 ℃

Life time                10y @ 25       △C Within ±30% of initial measured value ℃

ESR Within 2 times of initial specified value

Cycle Life              500k cycles @ 25 △C Within ±30% of initial measured value ℃

ESR Within 2 times of initial specified value

Cycle: between specified voltage and half voltage under constant current at 25℃

Dimensions

| D | L |
| --- | --- |
| 35 | 60 |

Standard RatingsL d F a

| Rated Cap(F) | Size mm | Internal Resistance （mΩ） | LC (mA) | Stored Energy | Specific Energy | Specific power | Max. Current | ISC | Weight | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Measure At 25℃ | ΦDXL | AC (1KHz) | DC | 72Hrs 25℃ | Wh | Wh/kg | Wh/L | Pd W/kg | Pmax W/kg | 1s to 1/2V(A) | (A) | (g) | SNL2R73673560 |
| 360 | 35*60 | 7 | 13 | 1.00 | 0.3645 | 5.5227 | 6.3174 | 1020 | 3945 | 85.563 | 208 | 66 |  |